General

Andrepol Topcoat P18 is a pre-accelerated unsaturated polyester resin topcoat based on isophthalic acid and neopentyl glycol. It is available both sprayable and brushable. The topcoat has excellent chemical resistance, high heat resistance and high elongation at break.

It is used in chemical tank construction, electroplating tanks, swimming pools, tank construction, etc.

The topcoat corresponds to resin group 3 according to DIN 18820.

Chemical and physical properties :

Value		Unit			Method

Acid value			18 maxmg 	KOH/g		ASTM D 1639

Appearance			colourless or coloured

Stability at 65°C		6		days			SIR 10242

Gel time at 25°C

100 g resin

1.5 g MEKP 50%10-20		min			ASTM D 2471

Consumption			500-700g/m²

Spec. properties of the topcoat

Value		Unit			Method

Barcol hardness			45					ASTM D 1706

Flexural strength		100		MPa			DIN 53452

E-modulus			3500		MPa			DIN 53452

Tensile strength			75		MPa			DIN 53455/ EN 61

E-modulus			3700		MPa			DIN 53455/ EN 61

Elongation at break			3		%			DIN 53455/ EN 61

HDT				100		°C			ISO 75A

Packing

The product is available in tin packaging of 1; 5; 10; 30 kg, in 225 kg drums and

1000 kg container delivered.

Storage and shelf life

The product must be stored in a cool, dark place, free from iron and copper salts as well as organic and inorganic peroxides, and dry, sealed in its original packaging.

When stored in this way, the resin will keep for at least 6 months.

Security

the product is highly flammable and harmful to health. For further information, please refer to the safety data sheet.